MMFX Steel Dowel Bars & Tie Bars

MMFX 2 pavement dowel bars shall conform to the following:

- Steel pavement dowel bars shall be manufactured of MMFX 2 Steel, as applied by MMFX Steel Corporation. Steel pavement dowels shall conform to the ASTM A1035 specification for chemical and mechanical requirements.

- MMFX 2 steel pavement dowel bars shall be 18-inches in length and [1.25] [1.5] inches in diameter. For dimensional tolerances, MMFX dowel bars shall conform to ASTM A29 table A1.1 or A2.1.

- The surface of the finished cut to length MMFX2 dowels shall be provided with a hot-rolled, as-rolled finish including mill scale.

- The contractor shall furnish a Manufacturer’s Certificate of Compliance including mill test report verifying conformance to the aforementioned specifications.

- For tie bars #5 MMFX 2 reinforcement bars 30” in length will be specified.